## Slide 1: Computation Chemistry
Lecture 11: Electronic Structure in Periodic Systems

## Slide 2: Bravais lattices
Bravais lattices: the distinct lattice types which when repeated can fill the whole space
Wigner-Seitz cell: the most compact cell
First Brillouin zone: the Wigner-Seitz cell of the reciprocal lattice
2D Example:
Five distinct types of Bravais lattices
http://iopscience.iop.org/article/10.1088/0143-0807/35/5/055021

## Slide 3: Bravais lattices
Bravais lattices: the distinct lattice types which when repeated can fill the whole space
Wigner-Seitz cell: the most compact cell
First Brillouin zone: the Wigner-Seitz cell of the reciprocal lattice
2D Example:
reciprocal lattice
real lattice
Reciprocal lattice:

## Slide 4: Bravais lattices-3D
http://www.xtal.iqfr.csic.es/Cristalografia/parte_03_4-en.html
14 distinct types of Bravais lattices
7 crystal systems
4 types of centering

## Slide 5: Bravais lattices-3D
14 distinct types of Bravais lattices
7 crystal systems
4 types of centering
Reciprocal lattice and the first Brillouin zone
Cubic Example:
FCC Example:
Computational Materials Science 49 (2010) 299–312

## Slide 6: Bloch’s Theorem
Bloch's theorem: the wavefunction of an electron within a periodic potential can be written as the product of a lattice periodic part and a wavelike part:
i: the band index
k: a continuous wavevector that is confined to the first Brillouin zone of the reciprocal lattice
has the same periodicity as the direct lattice, it can be expressed in terms of a discrete plane-wave basis set with wavevectors, that are reciprocal lattice vectors of the crystal, i.e.
The above results show that the electron wavefunctions can be expanded in terms of a linear combination of plane-waves:

## Slide 7: Bloch’s Theorem
Real space lattice: R = n1 a1+ n2 a2+ n3 a3
Reciprocal space lattice: G = n1 b1+ n2 b2+ n3 b3
First Brillouin Zone: k = kx b1+ ky b2+ kz b3
Electron wavefunctions:

## Slide 8: Bloch’s Theorem
Plug into Kohn-Sham equation:
Kinetic energy:
Potential energy:
Integral in k space:
Integration over all k in the first Brillouin zone. This integration cannot be done analytically.
k-point sampling